# Synthesis, structural investigation, dielectric and magnetic properties of Zn2+2+-doped cobalt ferrite by the sol–gel technique

Mohammad Sajjad Hossain           Md. Badiul Alam                    Mohammad Shahjahan

Most. Hosney Ara Begum              Md. Moazzem Hossain         Suravi Islam

Nazia Khatun                                 Mukul Hossain                       Mohammad Saiful Alam

Md. Al-Mamun

## Abstract

Zinc substituted cobalt ferrite nanoparticles with elemental composition Co1−x1−xZnxFe2O4 (x=0.0x=0.0, 0.2, 0.4, 0.6) were prepared by the sol-gel auto-combustion technique using Co, Fe, Zn nitrate as a precursor where nitrates to citrate was 1:3. The as prepared powder of cobalt zinc ferrite was sintered at 900∘C for 3h. Structural, morphological, dielectric and magnetic properties were studied by x-ray diffractometer (XRD), scanning electron microscope (SEM), high precision impedance analyzer and vibrating sample magnetometer (VSM), respectively. The peaks obtained from the XRD confirmed samples having crystallite (∼∼32–36nm) single phase inverse spinel structure without any traceable impurity. Lattice parameters were calculated from XRD and it increases with Zn content. SEM revealed irregularly shaped grains (∼0.5∼0.5–0.7μμm) morphology with heterogeneous distribution. The dielectric constant (ε′ε′) and dielectric loss (tanδtanδ), have been measured as a function of frequency at room temperature. The dependence of ε′ε′ and tanδtanδ with frequency showed the normal dielectric behavior in accordance with the Maxwell-Wagner type of interfacial polarization and electron hopping change between Co2+2+ and Co3+3+ as well as between Fe2+2+ and Fe3+3+ ions at octahedral sites.